Product Description

Premium quality electrical self-extinguishing soft PVC tape with a rubber adhesive

Applications

Predominantly electrical insulation, also colour coding and for electrical cables wrapping in automotive application.

Features & Benefits

Good resistance to abrasion, corrosion and moisture

High dielectric strength

Excellent conformability

Conforms to BS3924 replaced by EN 60454-3-12:2006

Conforms to EN 60454-3-12:2006

IEC 62321:2008

2006/95/EC (Low Voltage Directive)

UL510 certificated (Flame Retardant)

Technical Performance

| Description | Units | Value | Test Method |
| --- | --- | --- | --- |
| Total thickness | mm | 0.13±0.005 | GB7125-1999 |
| Adhesive | - | Rubber | No residue |
| Elongation at break | % | ≥180 | GB7753-1987 |
| Tensile strength | N/cm | ≥22 | GB7753-1987 |
| Voltage breakdown | KV | 6 | EN 60454-4-3-12:2006 |
| Flammability | - | PASSED | UL510 |

Declaration of Conformity Information

EN 60454-3-12:2006, IEC 62321:2008, 2006/95/EC (Low Voltage Directive) BS3924, UL510

RoHS Compliance Status

2011/65/EU

Storage Details

Shelf life recommended 2 years from date of despatch at the moderate temperature and humidity environment.