Product Description

Silicone rubber electrical tape is a high-temperature arc and track resistant tape composed of self fusing, inorganic silicone rubber that is easy to tear and remove from liner.

Applications

Used for Automotive, Marine, Electrical, Plumbing, insulating and general purpose applications including water hose & pipe repairs, weatherproofing electrical connections and fitting, bundling wires, boat rigging, sport & tool handles, plumbing repairs, rope ends, and emergency radiator hose repair O-Rings & seals.

Features & Benefits

Excellent arc and track resistance

High dielectric strength

IEC 60085 Class 180 insulator (Class “H” insulator)

Halogen free

Excellent conformability

Instantaneous fusion no needs to hold in place

Technical Performance

| Description | Units | Value | Test Method |
| --- | --- | --- | --- |
| Total thickness | mm | 0.5mm |  |
| Operating temp | °F | -130 to +500 | Continuous |
| Dielectric strength | vpm | 400 | ASTM D149 |
| Dielectric constant | 1KH³ | 2.95 | ASTM D150 |
| Dissipation factor | 1KH³ | <0.0004 | ASTM D150 |
| Volume resistivity | OHMS/cm min | 1 x 10 | ASTM D257 |
| Water absorption | % Max. by weight | 3 | FED, STD 601, method 6251 |
| Tensile strength | PSI | 700 | ASTM D412 |
| Elongation | % | 300 | ASTM D142 |

Declaration of Conformity Information

WRAS Approved to BS6902-1 (2000) – See file for certificate

REACH SVHC Status contains Boric Acid (CAS 10043353, EINICS 233-139-2)

RoHS Compliance Status – Yes

Storage Details

Shelf life recommended 5 years from date of manufacture at the moderate temperature and humidity environment.